|  | PRESS RELEASE |
| --- | --- |

CTIA detected a battery-operated toy "Pistole LN 320/305" posing a serious risk

(Prague, 15 April 2024) The Czech Trade Inspection Authority (CTI) has found a product in the domestic market that poses a serious risk to the environment. The product in question is the battery-operated toy 'Pistole LN 320/305'.

It is a plastic gun-shaped toy with 2 x AA batteries, intended for children from 3 years of age. The toy was sold in a transparent plastic container with a label with the toy's identification and maintenance information. Tests performed by the Testing Laboratory No. 1004, ITC, a. s., confirmed a significant non-compliance with the requirements of Government Order No. 481/2012 Coll., on the restriction of the use of certain hazardous substances in electrical and electronic equipment, based on Directive 2011/65/EU-RoHS. The solder joint inside the toy was found to have a lead content exceeding the permitted limit value of 0.1% by a factor of up to 73.7%. Failure to comply with the requirements of the current legislation poses a serious environmental risk due to potential environmental pollution.

The required CE marking was not indicated directly on the product. The complete identification data of the manufacturer and the importer were not affixed on the product or on the packaging. The inspected product thus fails the requirements of Government Regulation No 86/2011 Coll., on Technical Requirements for Toys, as well as Government Regulation No 481/2012 Coll., on the restriction of the use of certain hazardous substances in electrical and electronic equipment.  In order to prevent further occurrence of identical products in the market that do not comply with the requirements of Directive 2011/65/EU - RoHS, as far as the maximum permissible lead content in the components of electrical toys is concerned, the Czech Trade Inspection Authority imposed a protective measure on the distributor pursuant to Section 18a(3) and (4) of Act No. 22/1997 Coll., on Technical Requirements for Products, as amended, consisting in a ban on distribution and withdrawal of the above-mentioned product from the market. The product was reported to the MIT contact point and information about it was published in the Safety Gate system.

Product information:

Name:			not displayed

Model number:		LN 320/305

EAN:			6008154142397

Manufacturer:		not displayed

Importer:		„L&N“

Distributor:		Thi Thanh Binh Nguyen, Kadaňská 2349/4, 430 03 Chomutov

Country of origin:		Čína

Pictures of the product