|  | PRESS RELEASE |
| --- | --- |

CTIA detected a battery-operated toy "Electronic Keys" that poses a serious risk

(Prague, 11 April 2024) In the Czech market, the Czech Trade Inspection Authority (CTIa) found a product which poses a serious risk to the environment. The product is named the battery-operated toy 'Electronic Keys'.

It is a plastic toy with AA 4 x 1.5 V batteries shaped like electronic keyboard, intended for children over 3 years old. The toy has 31 keys, 6 demo versions, 8 tones, etc. The toy is sold in a paper box with written information marked on it.  Tests carried out by the Testing Laboratory No. 1004, ITC, a. s., confirmed significant non-compliance with the requirements of Government Order No. 481/2012 Coll., on the restriction of the use of certain hazardous substances in electrical and electronic equipment, based on Directive 2011/65/EU-RoHS. On the soldered joint inside the toy, multiple exceedances of the lead content up to 66 % against the permitted limit value of 0.1 % and multiple exceedances of the cadmium content up to the values of 0.0661, 0.0558, 0.0367 % (depending on the place of measurement) against the permitted limit value of 0.01 % were found. Failure to comply with the requirements of the legislation in force poses a serious environmental risk due to possible pollution of the environment.

The required CE marking was not indicated directly on the product (the marking was not attached inseparably). In addition, the product did not bear the identification data of the product, the manufacturer and the importer. The inspected product thus does not comply with the requirements of Government Regulation No 86/2011 Coll., on Technical Requirements for Toys, as well as Government Regulation No 481/2012 Coll., on the restriction of the use of certain hazardous substances in electrical and electronic equipment. In order to prevent further occurrence of identical products in the market that fail the requirements of Directive 2011/65/EU - RoHS as regards the permitted limit of lead and cadmium content in components of electrical toys, the Czech Trade Inspection Authority imposed a protective measure on the distributor pursuant to Section 18a(3) and (4) of Act No. 22/1997 Coll., on Technical Requirements for Products, as amended, which is a ban on distribution and recall of the above-mentioned product from the market. The product was reported to the contact point at the MIT and information about it was published in the Safety Gate system.

Product information:

Trademark:		not displayed

Model type:		21P952

EAN:			6949115103333

Manufacturer:	Jinjiang Shengle Electronic Technology Co., LTD., No. 1019, Xingan Road, Tonglin Village, Anhai Town, Jin Jinjiang, Quanzhou City, Fujian Province, Čína

Importer:		SPARKYS, HM Studio, a. s., Průmyslová 504, 250 70 Postřižín

Distributor:		Libor Všetečka, Na Pakšovce 2207, 397 01 Písek

Product origin:		China

Pictures of the product