|  | PRESS RELEASE |
| --- | --- |

CTIA detected a battery-operated toy "Pistole 78090" in the market posing a serious risk

(Prague, 12 April 2024) The Czech Trade Inspection Authority (CTIA) detected a product in the internal market that poses a serious risk to the environment. This product is the battery-operated toy 'Pistole 78090'.

It is a plastic gun-shaped toy, intended for children from 3 years of age. The toy contains non-replaceable batteries. It was sold in a transparent plastic packaging and with an affixed paper label with information on the use of the product.

Tests carried out by Testing Laboratory No. 1004, ITC, a. s., confirmed a major non-compliance with the requirements of Government Order No. 481/2012 Coll., on the restriction of the use of certain hazardous substances in electrical and electronic equipment, based on Directive 2011/65/EU-RoHS. It was detected that a solder joint inside the toy contains multiple exceedances of the lead content up to 77.9% when compared to the permitted limit value of 0.1%, and cadmium up to 0.1812% when compared to the permitted limit value of 0.01%. Such failure to comply with the legal requirements in force poses a serious environmental risk due to possible pollution of the environment.

The required CE marking was not indicated directly on the product. The inspected product thus does not comply with the requirements of Government Order No 86/2011 Coll., on Technical Requirements for Toys, as well as Government Order No 481/2012 Coll., on the restriction of the use of certain hazardous substances in electrical and electronic equipment.  In order to prevent further occurrence of identical products in the market that do not comply with the requirements of Directive 2011/65/EU - RoHS, as regards the permitted limit of lead and cadmium content in electric toy components, the Czech Trade Inspection Authority imposed a protective measure on the distributor pursuant to Section 18a(3) and (4) of Act No. 22/1997 Coll., on Technical Requirements for Products, as amended, which is a ban on distribution and withdrawal of the above-mentioned product from the market. The product was reported to the contact point at the MIT and information about it was published in the Safety Gate system.

Product information:

Name:			Pistole 78090

Model number:		78090

EAN:			8592117780903

Manufacturer:	HK WENO TOYS CO., LIMITED, DongGuaHu Industrial, Lianxia town, Chenghai district, Shantou City, Guangdong Province, China

Importer:		Mikro Trading a.s., Podivín 991, 691 45, Česká republika

Distributor:		YourShop s. r. o., Mírové Náměstí 54, 384 11 Netolice

Product origin:		China

Picutres of the product