|  | PRESS RELEASE |
| --- | --- |

The battery-powered toy "AKU drill T1401" poses a serious risk to the environment

(Prague, 16 May 2024) The Czech Trade Inspection Authority has found that a product on the internal market poses a serious risk due to possible environmental pollution. The toy in question is a battery-operated toy "AKU drill T1401". The CTIA imposed a protective measure on the distributor, which is a ban on distribution and withdrawal of the product from circulation.

Battery toy „AKU vrtačka T1401“

Značka:			             TEGOLE

Číslo modelu: 	T1401

EAN:	8 5 9 2 1 9 0 1 2 4 0 8 3

Výrobce:	TEGELI TOYS FACTORY, WAIPU NEW INDUSTRIAL AREA, FENGXIN 3rd ROAD, CHENGHAI DISTRICT, SHANTOU CITY, GUANGDONG PROVINCE, CHINA

Dovozce: 	TEDDIES s.r.o., Česká 151/16, 602 00 Brno, Česká republika

Distributor:	Megahračky s.r.o., Tovární 174, 381 01 Český Krumlov

Původ výrobku: 		             Čína

This is a plastic toy in the shape of a drill on AA 2 x 1.5 V batteries, designed for children over 3 years old. The toy was sold in a cardboard box with a plastic window, on which a label with information was glued.

Tests carried out by the testing laboratory confirmed significant non-compliance with the requirements of Government Regulation No. 481/2012 Coll., on the restriction of the use of certain hazardous substances in electrical and electronic equipment (Directive 2011/65/EU - RoHS). The solder joint inside the toy was found to contain multiple exceedances of the lead content up to 66,1 % against the permitted limit value of 0,1 % and cadmium up to 0,1153 %, 0,0534 % and 0,0543 % (depending on the place of measurement) against the permitted limit value of 0,01 %. Failure to comply with the requirements of the legislation in force poses a serious environmental risk due to possible pollution of the environment.

The complete identification data of the product, the manufacturer and the importer were not provided directly on the product. The inspected product therefore does not comply with the requirements of Government Regulation No 86/2011 Coll., on technical requirements for toys and Government Regulation No 481/2012 Coll., on restriction of the use of certain hazardous substances in electrical and electronic equipment.

In order to prevent further occurrence of identical products on the market that do not comply with the requirements of Directive 2011/65/EU - RoHS as regards the permitted limit of lead and cadmium content in components of electrical toys, the CTIA imposed a protective measure on the distributor pursuant to Section 18a(3) and (4) of Act No. 22/1997 Coll., on technical requirements for products, as amended, which is a ban on distribution and withdrawal of the product from circulation. The product was reported to the contact point at the MIT and information about it was published in the Safety Gate system.