|  | PRESS RELEASE |
| --- | --- |

Battery-powered toy "FORD GT POLICE CAR" poses a serious risk to the environment

(Prague, 9 July 2024) The Czech Trade Inspection Authority found a product in the internal market posing a serious risk to the environment. The product in question is the battery-powered toy "FORD GT POLICIE". The CTIA imposed a ban on its distribution and its withdrawal from circulation.

Battery-powered toy „Auto FORD GT POLICIE“

Trademark:		XTR TOYS

Model No:		61367

EAN:			8592117613676

Manufacturer:	OKK Trading, Inc, 2018, Made in Shantou, China

Importer:		Mikro Trading a. s., Podivín 991, 691 45 Podivín

Distributor:		PRIOR ČESKÁ REPUBLIKA s. r. o., Lannova tř. 1461/22, České Budějovice

Product origin:		China

This is a plastic toy, battery-powered car with a power supply of 3 x AG 13, intended for children over three years of age, in a paper box with a plastic window, on which information for use and warnings were provided.

Tests carried out by Testing Laboratory No. 1004, ITC, a. s., confirmed a significant non-compliance with the requirements of Government Regulation No. 481/2012 Coll., on the restriction of the use of certain hazardous substances in electrical and electronic equipment, based on Directive 2011/65/EU-RoHS. According to the findings, on the soldered joint inside the toy the lead content exceeded the permitted limit value of 0.1% by up to 76.9% and the cadmium content exceeded the permitted limit value of 0.1732% by up to 0.01%. Failure to comply with the requirements of the legislation in force poses a serious environmental risk due to possible pollution of the environment.

The required CE marking has not been affixed directly to the product. In addition, not all the required information on the product, the manufacturer and the importer was provided on the product. Some information for use and warning information was not provided in the Czech language. The inspected product thus does not comply with the requirements of Government Regulation No. 86/2011 Coll., on Technical Requirements for Toys, and Government Regulation No. 481/2012 Coll., on the restriction of the use of certain hazardous substances in electrical and electronic equipment.

In order to prevent further occurrence of identical products in the market that fail to comply with the requirements of Directive 2011/65/EU - RoHS in terms of the permissible limit of lead and cadmium content in components of electrical toys, the Czech Trade Inspection Authority imposed a protective measure on the distributor pursuant to Section 18a(3) and (4) of Act No. 22/1997 Coll., on Technical Requirements for Products, as amended, which is a ban on the distribution and withdrawal of the above-mentioned product from circulation. The product was reported to the contact point at the Ministry of Industry and Trade and the information about it was published in the Safety Gate system.

Photo documentation of the product